Town of Phillipsburg, Inspections

Sidewalk/Driveway Permit Application

Applicant:  This questionnaire must be filled out and accompany your application for a construction permit.  Please read the abbreviated minimum requirements and answer the pertinent questions below.

SIDEWALK:

- All sidewalks to be demolished shall be excavated to a minimum depth of 8” below proposed finished grade elevation.

- Subase shall be constructed of 4” Type 57 clean crushed stone ¾” or smaller.  Stone shall be compacted.

- Concrete shall be a minimum thickness of 4” with 28-day compressive strength of 3,000 psi for sidewalks.  *Driveway aprons shall be minimum thickness of 6” with strength of 3,500 psi.  (wire mesh optional)

- Surface finish shall be very light hair broom or wood float.

- Contraction joints @ 5” intervals 1” deep by ½” wide.  Expansion joints @ 10’ intervals, minimum ½” thick pre-molded material or prefabricated metal.

- Curing shall be done with burlap or plastic sheeting for a minimum period of 72 hours.

- Form inspection required prior to pouring concrete.

SIDEWALK/DRIVEWAY QUESTIONS:

1.	Length of walk to be constructed:		       _____________L.F.

2.	Existing planting Strip?			       ________Yes ________No

3.	Is curb to be reconstructed? 		       ________Yes ________ No

4.	Length of Curb if to be done:		       _____________L.F.

5.	Is the driveway apron to be done?                 ________ Yes ________ No

6.	Driveway apron width? 	                  	       _____________L.F.

7.	Type of Expansion Material? (Check one)    _______Bitumen _______Metal

8.	Surface finish?	(Check one)                 ________Broom ________Float

9.	Driveway plan attached? (New only) 	      ________ Yes ________ No

I have received from the Town all necessary specifications for sidewalk construction and intend to comply with the same.

______________________________								        Owner/Agent